Study the effects of calcinations and evolution of crystallographic parameters of two Tunisian natural phosphates

A.CHAABOUNIa, C.CHTARAb, A. NZIHOU C, H. EL FEKIa

aLaboratory of sciences of materials and environment, Faculty of Sciences of Sfax, Sfax, Tunisia.

Soukra Road km 4 - B.P. n° 802 - 3038 Sfax

E-mail:ahmed_chfss@yahoo.fr

bTunisian Chemical group, Gabes, Tunisia.

Tunisian Chemical Group Research Directorate Z.I. BP72 - 6000 - GABES

E-mail:chaker.chtara@gmail.fr

cEngineering School of Mines of Albi-Carmaux, Toulouse, France.

Engineering School of Mines of Albi-Carmaux RAPSODEE Centre Campus Jarlard 81013 Albi CT Cedex 09

E-mail:ange.nzihou@mines-albi.fr

aLaboratory of sciences of materials and environment, Faculty of Sciences of Sfax, Sfax, Tunisia.

Soukra Road km 4 - B.P. n° 802 - 3038 Sfax

E-mail:hafed.elfeki@yahoo.fr

Corresponding author: Hafed El Feki, Prof., research fields: materials sciences and environment. Faculty of Sciences of Sfax, Tunisia. Email:hafed.elfeki@yahoo.fr. Telephone: +216 98 66 75 58, fax numbers: +216 74 67 48 10. ORCID: 0000-0001-8508-3586.

Abstract

Tunisian natural phosphate is a highly form of fluorapatite, carbonate fluorapatite, also known                            as “francolite”. The presence of carbonate in mineral phosphates influences their reactivity overlooked acid attack, but their presence requires a supplementary adding of sulfuric acid in the plants of production of phosphoric acid; and causing the formation of foams in the reactors during the addition of sulfuric acid. The presence of carbonates             in high contents reduces the price value of phosphate rock.

We propose in this work to study thermally the decomposition of two carbonated fluorapatite                      in a range of temperature between ambient and 1000°C; and the variation of the value of crystallographic parameters of the two samples of phosphate. The X-ray diffraction technique is used for this mineralogical study.

By referring to the crystallographic parameters of the lattice of phosphate, we note that the increase                     in temperature decarbonated the francolite which is transformed largely to a fluoroapatite. In addition,                           it was reported that the first decarbonation is around 650°C translated the kinetics of decomposition of                          the carbonate ions of the type B associated with a vaccum, while the second decarbonation is around 1000°C                    and related to the thermal decomposition of the entity of CO3F, generated by the decomposition of carbonate ions of    type B and A. The presence of these ions would be the result of a reorganization of the crystal lattice.

Keywords: Effect of Calcinations, Tunisian natural phosphate, Carbonated fluoroapatite, Mineralogical study, X-ray diffraction.

1. Introduction

Tunisian natural phosphate is an essential element used in the plants of production of phosphoric acid. It is a highly form of fluorapatite, carbonate fluorapatite, also known                        as “francolite” [1-3]. The structure of apatite can be described in terms of an approximate hexagonal close packed set of spheres in which each sphere represents a tetrahedral PO43- ion.              It is well established that carbonate substitution has a destabilizing effect on the apatite structures resulting in increased solubility [2-4]. In addition, the presence of carbonates in the mineral phosphates greatly influences their reactivity towards acid attack [5]. The presence of carbonates requires a supplementary add of sulfuric acid during the production of phosphoric acid;                      in addition to it causes foaming which inhibits the cooling of the reaction. Accordingly                      an increasing in temperature and viscosity of the phosphoric slurry; which leads to the formation of the hemihydrate phosphogypsum, it results a bad filtration which affects the quality of                  the phosphoric acid product and decreases the chemical yield [6-8]

Apatites have the general formula, Ca10(PO4)6X2 where X is typically F (fluorapatite, FAp), OH (hydroxyapatite, OHAp), or Cl (chlorapatite, ClAp). The apatite lattice is very tolerant of substitutions, vacancies and solid solutions, for example, X can be replaced by ½CO3 or ½O; Ca by Sr, Ba, Pb, Na or vacancies; and PO4 by HPO4, AsO4, VO4, SiO4 or CO3 [9].

Beneficiation by calcinations is one of the well known processes. It is based                            on the dissociation of the calcium carbonate by thermal energy. Depending on the efficiency of the process, calcinations may lead to almost complete disposal of the carbonates present                          in the phosphate rock [10-12].

There are two types of carbonate apatite:

The carbonate apatite of type A in which CO32- ions are fixed along the senaire helical axis where usually located the monovalent anions [13-14].

The  carbonate apatite of type B in which CO32- ions occupied the sites of phosphate ions [13, 15-17] with creation for each substitution, a lacuna in a calcium site and the other in oxygen site              and the third in the tunnels site.

It is noted that the crystallographic parameter "a" of carbonated hydroxyapatites containing sodium ions increases by adding carbonates content, while parameter "c" decreases [10, 12-14].

In this work, we studied the temperature of calcinations and its effects on two sedimentary phosphates in a range of temperature between ambient and 1000°C and the effect of this increase on the crystallographic parameters “a” and “c” of these two samples.

2. Experimental procedure

The tests are performed on the laboratory scale in an adjustable furnace in temperature on                the Tunisian phosphate. The study of the time of calcinations is carried out by introducing samples of phosphate in the furnace for a period of 60 minutes at a fixed temperature (250°C, 650°C and 1000°C).

The powders were characterized by X-ray diffraction (DRX). The diffractograms are acquired with the radiation Kα of Copper (CuKα and the wavelength is λ = 1,541 Å) using                                 a diffractometer SIEMENS D5000. Besides, the structural information was obtained starting from a powder diagram collected in the angular field 5–110 in 2h with an angular step of 0.04° (2h) and counting time of 5 s. The refinement of the lattice parameters is achieved by WPF method (Whole Pattern Fitting or Le Bail method) using Fullprof Suite software version 1.10.

3. Results and discussion

The X-ray diffractograms are shown in figure 1 and Figure 2.

Fig. 1. X-Ray diffractograms of the sample of phosphate 1 at different temperatures (ambient temperature, 250°C, 650°C and 1000°C).

Fig. 2. X-Ray diffractograms of the sample of phosphate 2 at different temperatures (ambient temperature, 250°C, 650°C and 1000°C).

The diffractograms of phosphates presents fine lines. The analysis of this diagram                    by isotopy with the charts of reference [18, 19] show that the solids crystallize in the hexagonal system and have P63/m symmetry. The crystallographic parameters of phosphate rocks and those of references [18, 19] are shown in table 1.

| Table 1: Crystallographic parameters of phosphate rocks and those of references. |
| --- |
| Parameter | Phosphate 1 | Phosphate 2 | Hydroxy-Ap | Fluoro-Ap | Francolite |
|  |  |  | [18, 19] | [18, 19] | [18, 19] |
| a | 9.327 | 9.337 | 9.421 | 9.372 | 9.360 |
| b | 9.327 | 9.337 | 9.421 | 9.372 | 9.360 |
| c | 6.894 | 6.909 | 6.882 | 6.888 | 6.890 |

At room temperature, by comparison between the crystallographic parameters of                   the two samples of phosphates and those of references (a = 9,327 Å for the sample of                phosphate 1, and a = 9,337 Å for the sample of phosphate 2) and those hydroxyapatite                          (a = 9.421 Å), fluoroapatite (a = 9.372 Å) and the francolite (a = 9.360 Å). This proves that               our fluorapatite is carbonated and it is a francolite [18, 19].

The calculation of the crystallographic parameters of each sample at various temperatures                  and which are recapitulated in table 2 and table 3, shows that the volume of the crystallographic                      mesh of the crude phosphate 2 (V = 521,733 Å3)is larger than that of crude phosphate 1                       (V = 519,294 Å3); this is explained by the presence of much more OH- ions than of  F- ions                 in the crude phosphate 2 than in the crude phosphate 1, knowing that the ionic F- ray (1,33 Å)             is smaller than the ionic ray of OH- (1,43 Å).

| Table 2: Evolution of crystallographic parameters according to the temperature of the sample of phosphate 1 |
| --- |
|  | Crude phosphate 1 | Phosphate 1 - 250°C | Phosphate 1 - 650°C | Phosphate 1 - 1000°C |
| Temperature (°C) | 25 | 250 | 650 | 1000 |
| a (Å) | 9,327 | 9,3507 | 9,2912 | 9,3809 |
| b (Å) | 9,327 | 9,3507 | 9,2912 | 9,3809 |
| c (Å) | 6,894 | 6,927 | 6,8571 | 6,8868 |
| ( (degrees) | 90 | 90 | 90 | 90 |
| b (degrees) | 90 | 90 | 90 | 90 |
| γ (degrees) | 120 | 120 | 120 | 120 |
| Symetry | Hexagonal | Hexagonal | Hexagonal | Hexagonal |
| Space group | P63/m | P63/m | P63/m | P63/m |
| Volume ( Å3) | 519,294 | 524,523 | 512,643 | 524,852 |
| Bragg R-Factor | 0,353 | 0,148 | 0,0969 | 0,364 |
| RF-Factor | 0,188 | 0,19 | 0,163 | 0,543 |

| Table 3: Evolution of crystallographic parameters according to the temperature of the sample of phosphate 2 |
| --- |
|  | Crude phosphate 2 | Phosphate 2 - 250°C | Phosphate 2 - 650°C | Phosphate 2 - 1000°C |
| Temperature (°C) | 25 | 250 | 650 | 1000 |
| a (Å) | 9,33740 | 9,31680 | 9,33810 | 9,3858 |
| b (Å) | 9,33740 | 9,31680 | 9,33810 | 9,3858 |
| c (Å) | 6,9098 | 6,90110 | 6,90240 | 6,8954 |
| ( (degrees) | 90 | 90 | 90 | 90 |
| b (degrees) | 90 | 90 | 90 | 90 |
| γ (degrees) | 120 | 120 | 120 | 120 |
| Symetry | Hexagonal | Hexagonal | Hexagonal | Hexagonal |
| Space group | P63/m | P63/m | P63/m | P63/m |
| Volume ( Å3) | 521,733 | 518,779 | 521,252 | 526,057 |
| Bragg R-Factor | 0,762 | 0,811 | 0,779 | 0,284 |
| RF-Factor | 0,643 | 0,39 | 0,656 | 0,573 |

The representations of the crystallographic parameters according to the temperature are indicated on figure 3 and figure 4.

Fig. 3. Evolution of the crystallographic parameter “a” according to the temperature.

Fig. 4. Evolution of the crystallographic parameter “c” according to the temperature.

Calcinations are primarily intended to decarbonise and dehydration an ore with a high grade               in carbonates. During the heat treatment of mineral materials. Two solids capable of reacting giving to a monomolecular layer of the reaction product. The elements of the crystal lattice                are in oscillatory motion whose intensity increases with increasing temperature.                                   It is for this, the elements of the crystal lattice become able to overcome the force of attraction and change positions.

We note that there are fluctuations in parameters between ambient temperature and 250°C.              This is explained by a departure of the water of hydration and intercrystalline water [20, 21].

At the temperature 650°C, there is a carbon dioxide emission that begins to volatilize from 600°C to 800°C. This is a type B decarbonation which translates the kinetics of decomposition of                 the carbonate ions type B associated with a vaccum [22-25].

There is an emission of CO2 around 700°C that corresponds to the decomposition of CaCO3 presents in this powder of phosphate [22].

At the temperature 1000°C, there is a carbon dioxide emission that begins to volatilize from 800°C to 1050°C [23-25]. This is a type A and B decarbonations. This is a result of thermal decomposition of the entity CO3F generated by the decomposition of carbonate ions type A               and B [23-25]. decarbonation of sites B which is accompanied by the appearance of CaO due to the restructuring of the crystal lattice [23-25]. At 1000°C, by comparison between                              the crystallographic parameters of the two samples of phosphates (a = 9,3809 Å for the sample of phosphate 1, and a = 9,3858 Å for the sample of phosphate 2) and those hydroxyapatite                   (a = 9.421 Å), fluoroapatite (a = 9.372 Å) and the francolite (a = 9.360 Å). This proves that after decarbonation, our francolite is similar to the fluoroapatite [18, 19].

4. Conclusion

The heat treatment, in general and in the phosphate industry particularly is used in order to the valuation of raw ores, in their transformation into useful products, or even to transform raw materials into products directly.

The crystallographic parameters change depending on the temperature, which is the result of dehydration, and decarbonation type A or type B.

Calcinations decrease the content of Carbonates in the samples of phosphate. Accordingly it allows decreasing the consumption of sulfuric acid (H2SO4) during the production of phosphoric acid. Calcination gives therefore a product that fulfils the requirements of its use.

References

[1] McConnell D (1973) Apatite: its Crystal Chemistry, Mineralogy, Utilization, and Geologic and Biologic Occurrences, Springer-Verlag, Berlin.

[2] Jahnke RA (1984) The synthesis and solubility of carbonate fluorapatite. American Journal of Science 290, 58-78.

[3] CHAABOUNI A, CHTARA C, NZIHOU A & EL FEKI H (2013) Kinetic Study of the Dissolution of Tunisian Natural Phosphate or Francolite in Industrial Phosphoric Acid. Journal of Advances in Chemistry 6, 908-916.

[4] Chien SH & Black CA (1976) Free energy of formation of carbonate apatites in some phosphate rocks. Soil Science Society of America Journal 40, 234-239.

[5] Lehr JR, McClellan GH, Smith JP & Frazier AW (1972) Phosphates dans l'agriculture: Colloque international sur les phosphates minéraux solides, Toulouse.

[6] Becker P (1989) Phosphates and Phosphoric acid, Marcel Decker.

[7] SLACK AV (1968) PHOSPHORIC ACID, MARCEL DEKKER. INC, NEW YORK, Volume I, Part I, 129.

[8] Waggaman WmH (1953) PHSPHORIC ACID, PHOSPHATES AND PHOSPHATIC FERTILIZERS. SECOND EDITION, Second Printing, 183.

[9] Elliott JC (1994) Structure and Chemistry of the Apatites and Other Calcium Orthophosphates. Elsevier, Amsterdam.

[10] Memminger GG, Waggaman WH & Whitney WT (1930) The calcination or enrichment of phosphate rock. Journal of Industrial and Engineering Chemistry 22, 443–446.

[11] Kumar D (1980) Calcination of phosphate rocks. Chemie Ingenieur Technik 52, 736–740.

[12] Ozer AK (2003) The characteristics of phosphate rock in a fluidized bed for the upgrading. Advanced Powder Technology 14, 33–42.

[13] Bonel G (1972) Annales de Chimie (Paris) 7, 127-144.

[14] Trombe JC, Bonel G & Montel G (1967) Comptes Rendus de l'Académie des Sciences Series C 265, 1113.

[15] Legeros RZ (1967) Ph.D., Thesis, New York University.

[16] Legeros RZ, Legeros JP, Trautz OR &  Klein E (1964) Journal of Dental Research 43, 75.

[17] Vignoles C (1973) Thèse de 3ème cycle, Université Paul Sabatier de Toulouse.

[18] Young RA (1973) Colloque International CNRS, Paris 230, 21.

[19] Trombe JC (1973) Contribution à l'étude de la décomposition et de la réactivité de certaines apatites hydroxylées et carbonatées. Annales de Chimie 8, 251-269.

[20] LABARTHE JC, Bonel G & MONTEL G (1973) Annales de Chimie Paris 8, 289-301.

[21] Vignoles M (1984) Contribution à l’étude des apatites carbonatées de type B. Thèse d’état. Toulouse.

[22] Lafon JP,  Champion E & Assollant DB (2002) Caractérisation d'apatites phosphocalciques carbonatées. Matériaux.

[23] EL FEKI H, KHATTECH I, JEMAL M & Rey C (1994) Décomposition thermique d'hydroxyapatites carbonatées sodées.  Thermochimica Acta 237, 99-110.

[24] EL FEKI H, KHATTECH I & JEMAL M (1991) Décomposition thermique de fluorapatites carbonatées sodées. Journal de Chimie Physique 88, 1885-1892.

[25] EL FEKI H, Rey C & Vignoles M (1991) Carbonate ions in apatites: Infrared investigations in the ν4 CO3 domain. Calcified Tissue International 49, 269-274.